## Slide 1: Fatigue Design of Structures
G. Hénaff
1

## Slide 2: Damage tolerance

## Slide 3: Damage Tolerance
introduction

## Slide 4: DT Motivations
On Dec 22nd 1969, a F-111 fighter aircraft lost a wing during a training flight (2 pilots dead).
Origin of the failure: forging flaw introduced during the first processing operations but not detected at the time of manufacture
This accident triggered the largest survey ever conducted on a single material, in this case the D6AC steel but almost highlighte dthe need to take into account the presence of a flaw in the structure

## Slide 5: Standard Design
Simplified Wöhler curve
Reference loading R=0.1
Fatigue Quality Index (IQF):
Smax (R=0.1) at 105 cycles
R=0,1
Log (
s
max
)
R
s
max
(R)
s
max
(0,1)
Log (
N
)
10
5
p

## Slide 6: Standard Design (cont’d)
with

## Slide 7: Standard Design (cont’d)
M : influence of material ;
E : scale effect ;
T : influence of technological processes
T1 : influence of surface treatment ;
T2 : influence of mechanical treatment ;
  T 3 : influence of the type of joining for bolted or riveted assemblies ;
  T4 : Influence of adjustments for bolted joints .
Kt : stress concentration factor ;
C : Influence of the structural configuration (accidents of form, assemblies, lugs).

## Slide 8: Standard Design (end)

## Slide 9: Motivation
Target life
x 2
x 3
x 4
Full scale testing
Flaw size
Failure
Initial flaw

## Slide 10: Damage Tolerance
Objectives

## Slide 11: Objectives
Any structure must be able to withstand, at any time during its use, a limit load fixed during the initial design. Thus, an exceptional effort with a low probability is considered, but this should not lead to the ruin of the structure. The limit load will therefore be defined as the product of the exceptional effort by a safety factor (typically 1.5).
In the presence of cracks, the resistance is lower than the initial resistance estimated during design.
Damage tolerance thus determines the ability of a structure to withstand the presence of damage in the form of cracks without catastrophic consequences, even for exceptional effort until the damaged part is detected and repaired or the structure reaches the end of its life.

## Slide 12: Outputs
DT Analysis must provide:
the evolution of residual strength as a function of crack size;
the permissible crack size;
the propagation time from the detection threshold;
the permissible initial defect size in a new structure;
the interval of inspection or replacement.

## Slide 13: Tasks of the DT analysis
Define the range of use of the structure
Develop the spectrum of load factors
Identify critical points
Establishing the stress spectrum for each point
Identify the environment for each point
Establishing the cracking data

## Slide 14: Tasks of the DT analysis (cont’d)
Validate the crack growth analysis;
Determine the fracture toughness for each material and geometry;
Validate the residual resistance analysis methods;
Bring together all the partners concerned and collectively define the inspection methods and their periodicity

## Slide 15: DT Analysis
Propagation computation

a
Residual strength
Fracture toughness data
Kc
KIc
Thickness
K
Computation of SIF

t
Load spectrum
da/dN data
K
da/dN
R3 >R2 >R1
Time, number of flights
a
Fatigue life assesment

## Slide 16: DT assessment
Identification
of critical points
Geometry of defects
Damage detectability
Load spectrum
In-service measurements
Propagation calculations
Inspection period
Inspection interval
Field experience
Validation by tests on specimens
Update
DT assessment
DT analysis
Validation by tests on structural details and full-scale structure

## Slide 17: Damage Tolerance
Residual strength

## Slide 18: Residual strength
Regular loads (flight efforts)
Structural strength
Time
Limit load
VISUAL
NDT
Updated strength after repair
Extreme load
Inspection period

## Slide 19: Residual strength
Flaw size
Time
Inspection period
Inspection interval
Detection threshold
Critical flaw size

## Slide 20: Residual strength
H
Time
t1
t2
ai: initial flaw size
a0: NDT detection threshold
ai
a0
ap
Propagation Life
Flaw size
ap
Flaw size
ac
Residual strength
Initial resistance
max
 p

## Slide 21: Application
2
1
2
2
1
Multiple load paths
Crack arrester
Flaw size
Number of flights
Value at the limit load
Inspection period
Value of « sure » detection
element
1
element
2
element
1
Inspection period
Critical size at limit load
Critical size at limit load
Value at the limit load
element
2

## Slide 22: Application
Number of flights
Flaw size
Taille critique
à la charge limite
Value of « sure » detection
Critical size at limit load
Non damage-tolerant structure
To be assessed in safe life
Value of « sure » detection
inspection period
Damage Tolerant Structure with unique load path

## Slide 23: Toughness data as a function of thickness

## Slide 24: Residual strength of a panel
Residual strength f
Crack size a

## Slide 25: Residual strength of a stiffened panel
2 a
2r
2 a
2r
(a)
(b)
(c)
rivets
2a
2r

## Slide 26: Residual strength of a stiffened panel
Residual strength f
Crack size a
Non stiffened panel
Position of the stiffener
rivets
2a
2r

## Slide 27: Example of residual strength diagram

## Slide 28: Damage Tolerance
Different options

## Slide 29: Options
periodic inspections: repair if flaw detection;
"Fail Safe" design: repair if partial failure;
Leak Before Breakage Design: Pressure Vessels
Durability design: replacement or withdrawal after time H;
Proof test (destructive test): repair if rupture during the test.

## Slide 30: Periodic inspection
Flaw size
Sophisticated NDT techniques
Visual examination
Long inspection period BUT expensive NDT means
Fatigue life
Short inspection period BUT low cost NDT means
Damage
at the limit load

## Slide 31: Fail Safe

## Slide 32: Leak before breakage (LBB)
A
B
B
Through crack
2c
Wall thickness

## Slide 33: Proof test
N ou Time
a proof
a p
a d
(a)
s proof
s residual
(b)
(c)
s p
a proof
a p
Room Temperature
Low temperature
s proof
s residual
Nominal residual strength
Residual strength during proof test
a proof
Crack size
Crack size
a p
H

## Slide 34: Damage Tolerance
Calculation of propagation life

## Slide 35: Integration
Crack length, a
a

## Slide 36: Iterative computation
Initialisation
0;
N
;
a
a
0
j
=
=
j
i
a
a
=
÷
ø
ö
ç
è
æ
=
b
W
a
f
i
i
i
i
i
i
a
K
p
´
s
´
b
=
D
(
)
,...
R
,
K
F
dN
da
i
i
D
=
÷
ø
ö
ç
è
æ
(
)
example
for
mm
01
.
0
a
a
i
i
d
=
D
(
)
i
i
i
dN
da
a
N
D
=
D
i
i
j
N
N
N
D
+
=
i
i
j
a
a
a
D
+
=
(
)
continue
a
a
if
c
j
<

## Slide 37: AFGROW Flowchart

## Slide 38: Walker equation

## Slide 39: Walker equation

## Slide 40: Forman equation
McEvily - Forman

## Slide 41: NASGRO equation
The f function accounts for closure effects
Threshold function :

## Slide 42: NASGRO: closure

## Slide 43: NASGRO: Threshold
2024 T351

## Slide 44: NASGRO

## Slide 45: Sources of error
Error | Source | Comment | Factor on predicted fatigue life
LEFM Intrinsic Limitations |  | Small error for small cracks or small components | 1.1 - 2
Input data | KIc or Kc ou autre | Error on ap | 1.1-1.2
 | da/dN | Natural scatter | 1.1-1.5
 | Environment | Weight average | 1-2
 | Crack growth equation | Adjustment | 1.5
Assumptions | Crack growth direction (ex. LT vs SL) | Use of erroneous data | 1-2
 | Initial flaw size | Strong influence | 1-3
 | Shape | Surface flaws | 1-2
Stress Intensity Factor | Loads/Stresses | Measurements | 1-1.5
 |  | Analysis | 1-1.5
Load History | Sequence | Random or semi-random | 1.5
 | Truncation | Inadequate truncation | 1.1-1.3
Retardation | Model | Small if well calibrated | 1.1-1.3
 | Stress state | If not taken into account | 1.1-1.5
 | Yield strength | For example 10% too low | 1.5-2.0

## Slide 46: Example: crack growth in a lug
Procedure:
Consider an initial default size ai;
Determine the K in the screed for a = ai;
For this value read the corresponding crack growth rate;
Report the growth rate on the da / dN = f (a) diagram
The curve da / dN = f (a) must be integrated to obtain a = f (N)

## Slide 47: Example 2: stiffened panel
2024 T3, R=0.1
Crack initiated in the central bay

## Slide 48: Damage Tolerance
Variable amplitude loading - Retardation

## Slide 49: Load spectrum during a flight

## Slide 50: Spectrum of a F-18 fighter aircraft wing

## Slide 51: Standard load spectra

## Slide 52: FALSTAFF

## Slide 53: TWIST

## Slide 54: HELIX/FELIX
The distribution of cycles depends on the type of aircraft

## Slide 55: HELIX

## Slide 56: TURBISTAN

## Slide 57: TURBISTAN

## Slide 58: TURBISTAN

## Slide 59: Load history effects

## Slide 60: Markings on fracture surfaces

## Slide 61: Overload

## Slide 62: Retardation
a
N
S
(a) No retardation
a
N
(b) Retardation
S
da/dN
da/dN
(c) Delayed retardation
a
N
S
da/dN
da/dN
(c) Lost retardation
a
N
S

## Slide 63: Characteristic retardation parameters
a
N
S
aR
NR
da/dN
a
(da/dN)min
a*
S
(da/dN)0
aR
N0
NS

## Slide 64: Retardation mechanisms
The effect of residual stresses induced by the overload in front of the crack tip;
An increase in the crack closure effects induced by the material highly stretched during the overload and subsequently passed in the crack wake;
A crack tip blunting which would reduce the magnitude of stresses sustained at the crack tip assimilated to a micro-notch;
Crack tip hardening of the material induced by the overload.

## Slide 65: Overload/underload
a
N

## Slide 66: Wheeler model
ai
R0
bi
a0
Rpeak
Plastic zone interactions

## Slide 67: Willenborg model
ai
R0
Req
a0
Rpeak
KR: SIF required to create a PZ with a size Req defined by:
Retardation predicted if a load ratio effect is noticed on the da/dN curves.

## Slide 68: PREFFAS
P
t
n cycles
P
t
neq cycles
Pmax ref
Pmin ref
CAL equivalent sequence

## Slide 69: PREFFAS
At cycle i, the crack growth is given by:
ai = C x Keff m = C x (Kmax, i ‑ Kop,i)m
where C and m are the Paris law coefficients de la loi de Paris.
The value of Kop, i depends on the load history and is determined by a Elber relation :
Kmax, i ‑ Kop,i = U x (Kmax‑ Kmin)
With: U(R)=A x (Kmax, H / Kmin, H )+B
Where Kmin, H et Kmax, H are values representative of the load history.

## Slide 70: PREFFAS

## Slide 71: PREFFAS
The prediction of the propagation under variable amplitude loading therefore only requires the determination of 4 parameters:
  C and m, the coefficients of the PARIS law
  A and B, the coefficients of the ELBER relation
These 4 coefficients are derived from two tests
  1 under constant amplitude loading R=0.1
  1 under similar baseline loading with the introduction of an overload at  = 1.7 every 1000 cycles.

## Slide 72: PREFFAS

## Slide 73: PREFFAS

## Slide 74: PREFFAS
Pylon spectrum

## Slide 75: FASTRAN
(a) Max stress
as0
-as0
x
s
as0
-as0
x
s
-s0
(b) Min stress
W
c
r
x
Smax
y
W
c
w
x
Smin
y

## Slide 76: FASTRAN

## Slide 77: FASTRAN