## Slide 1: FATIGUE OF MATERIALS & STRUCTURES
G. Hénaff
1

## Slide 2: HIGH CYCLE FATIGUE

## Slide 3: Loading
σmax
Maximum stress
Stress
contrainte moyenne
σ
Stress range
Time
1 loading cycle
σa
Stress amplitude
σm

## Slide 4: Loading
Alternate Stress
Symetric alternate stress (R=-1)
Tensile alternate stress (R>0)

## Slide 5: Testing Machines
Electro-mechanical : low cycle fatigue (f < 1 Hz)
Servo-hydraulic : high cycle fatigue, propagation
(f <50 Hz)
Resonant :
high cycle fatigue, propagation
(100 Hz <f <200 Hz)

## Slide 6: Methodology
Fixed number of samples (geometry, surface);
Stress amplitude levels fixed prior to testing ⇒ number of test pieces tested per stress level;
For a given stress level, the distribution of lifetimes (number of cycles to failure) is determined.

## Slide 7: Isoprobability curves
Number of cycles N
σa
N
50
Isoprobability curve 50% of failure

## Slide 8: Wöhler Diagram

## Slide 9: Endurance diagram
10
2
10
4
10
6
10
8
Fatigue limit
s
D
s
e
t
s
a
s
a
s
e
s
a
R
m
Limited Endurance
Illimited Endurance
Low-cycle Fatigue

## Slide 10: Arbitrary fatigue limit
σa
N
107
σD
Aluminum alloys, stainless steels, fatigue corrosion: no asymptotic behavior ⇒ arbitrary definition of the fatigue limit for a given number of cycles (107 cycles, for example)

## Slide 11: Limited Endurance
About 105 to 107 cycles
Empirical relations:
  Weibull :
  Basquin :
  Bastenaire :

## Slide 12: -N curve
b
Basquin
Manson-Coffin
c
102
104
106
108
N
Nt : « Elastic-Plastic » transition

## Slide 13: -N curve

## Slide 14: Influence of Mean Stress
Smith-Watson-Topper:

## Slide 15: Influence of Mean Stress

## Slide 16: Influence of Mean Stress
Experimental observation: The permissible stress amplitude decreases when the mean stress increases
Taken into account by the use of abacuses (admissible stress as a function of the mean stress)→ Different representations.

## Slide 17: Haigh Diagram

## Slide 18: Influence of mean stress
R
e
R
m
A
B
Gerber
Goodman
Söderberg
s
a
s
m

## Slide 19: Goodman-Smith Diagram
σ
m
s
max
s
σ
a
s
min
A
B
s
R
e
R
m
45°
A
a
at =0

## Slide 20: Ros diagram
s
max
s
min
R=-1
R=-1/2
R=1/2
R=1
B
R=0
C
A

## Slide 21: Example: Goodman-Smith
Admissible stress amplitude Nf= 105 cycles and σm=200MPa ?
σmax~ 580 MPa
σmin~ -180 MPa

## Slide 22: Example: Haigh diagram
Admissible stress amplitude at R=0 with Nf=105 cycles?
sa=200
sm=200
smax=400

## Slide 23: Influence of loading mode
Tension
Rotative bending
Plane bending

## Slide 24: Scale effect
Determined on a reference sample with small dimensions
Observation : for a given stress amplitude value, the higher the dimensions of the testpiece, the lower the fatigue strength.
Causes :
  mechanical;
  probabilistic.
Scale effect coefficient :

## Slide 25: Scale effect: stress gradient
h1
h2
sn
Plane bending
sn
Difference in stress gradients:
  small thickness  high gradient. The less loaded layers support the highly loaded surface layers;
  high thickness  small gradient. All the surface layer are nearly loaded in a similar way  loss in fatigue resistance

## Slide 26: Scale effect: probabilistic aspect
The larger the dimensions of a component (volume, area), the more likely it is to have defects that behave as privileged initiation sites

## Slide 27: Influence of surface finishing

## Slide 28: Influence of surface finishing
Surface finishing factor:
with :
fatigue limit with the surface finishing under consideration ;
fatigue imit with a reference surface finishing.

## Slide 29: Residual stresses
Induced (on purpose or not) by:
  Inhomogeneous plastic deformations (especially in the vicinity of stress concentrators)
  Process
  Surface treatment (shot blasting, shot peening, coating,…)
  Expanded holes
  Joining

## Slide 30: Residual stresses near a stress concentrator
Plastic Zone
y 0,2%
+
-
After unloading

## Slide 31: Residual stresses induced by machining

## Slide 32: Burnishing
The residual stresses introduced by burnishing induce a higher fatigue resistance

## Slide 33: Expanded holes
Bore
Diameter of the pin larger than the diameter of the bore
sres
Pressure induced by the elastic medium
Plastic zone with compressive residual stresses
Before tension
After tension

## Slide 34: Influence of environment
The fatigue life is lower in an active environment (air) than in an inert environment (vacuum)
Related effect: influence of frequency