## Slide 1: FATIGUE OF MATERIALS & STRUCTURES
G. Hénaff
1

## Slide 2: Fatigue Crack propagation

## Slide 3: Opening modes
Opening
In-plane shearing
Out-of-plane shearing

## Slide 4: Standard specimens

## Slide 5: Compact tension specimen

## Slide 6: Fatigue crack propagation test
Pre-cracked specimens
Crack length monitoring of the crack length as a function of the number of aplled cycles (optical, compliance, potential drop)
Crack growth rate
Initiation

## Slide 7: Crack length monitoring
Optical method (direct)
Variation of Compliance
Potential drop (requires a calibration)
Extensometer
P
d

## Slide 8: Propagation curves
Slope da/dN
High 
Low 
a0
N
10000
20000
30000
40000
a

## Slide 9: Use of LEFM
Static or monotonic loading: the stress intensity factor accounts for the stress/strain field at the crack tip

## Slide 10: Use of LEFM
Idea: consider the stress intensity factor range K as the driving force for crack growth under cylic loading
NB: even when  is kept constant, K increases during crack growth

## Slide 11: Stress intensity factor

## Slide 12: LEFM concepts
Principle of similarity: a given value of K (for a wide variety of  and a values) induces the same cyclic stress/strain field at the crack tip, therefore the same damage and as a consequence the same crack growth rate
Crack growth rate
Initiation
Depends on specimen geometry, initial crack size, applied stress range, …

## Slide 13: Principle of similarity
Same da/dN range
da/dN
K
a0
Crack length a
da/dN
High 
Low 
Single curve
K - da/dN
Computation of K (,a)

## Slide 14: Paris correlation

## Slide 15: Transposability of laboratory data to structures

## Slide 16: da/dN-K curve
Crack growth rate at 50 Hz
1 mm/week
1 mm/day
1 mm/hour
1 mm/minute
m
I
II
III
10-11
10-9
10-7
10-5
da/dN
(m/cycle)
K
Influence of microstructure, load ratio
High
Weak
High

## Slide 17: Mechanisms

## Slide 18: Cyclic deformation at the crack tip
1
2
3
4
1
2
3
s
r
M
B
E
F
R
A
O
C
D
 y
-  y
“Elastic domain”
= 2y
e
 y
-  y
C
D
F
E
B
A
monotonic PZ
t

Far field loading

e
 y
-  y
elasto-perfectly plastic behaviour
4

## Slide 19: Cyclic plastic zone size
r
monotonic PZ :
cyclic PZ:
Example: at R=0, the cyclic PZ size is 4 times smaller than the monotonic PZ size.

## Slide 20: Propagation mechanisms: fatigue striations
Periodic markings on fracture surfaces;
Intermediate crack growth rate range (5x10-8 - 10-5 m/cycle);
Clearly defined in Aluminum alloys, much less in high strength alloys;
No striation in inert environment.

## Slide 21: Propagation mechanisms: fatigue striations
Striations afte fatigue at R=0.1 in a 2024 T351 alloy from the teardown of a A320 MSN004 wing: tip, maximum stress 400 MPa (a) and 300 MPa (b); engine area maximum stress 275 MPa (c) et 300 MPa (d) (Thèse F. Billy, ENSMA)

## Slide 22: Mécanismes de Propagation : Stries de Fatigue
Striations in a precipition-hardened martensitic stainless steel used in aerostructures (thèse L. Dimithe-Aboumou, ENSMA)

## Slide 23: Striation formation: Laird mechanism
t
s
t
s
t
s
t
s
t
s
t
s
Crack tip blunting
“Resharpening” of the crack tip

## Slide 24: Striation formation: Pelloux mechanism
2 cycles
2 cycles
Irreversible slip
(oxidation)
Reversible slip
(inert)
Dr. Regis Pelloux 1931 - 2015
→ Accounts for the absence of striation in vacuum

## Slide 25: Propagation mechanisms in the near-threshold region
More brittle aspect of the fracture surfaces(cleavage-like fracture, intergranular decohesions,….)

## Slide 26: Factors of influence

## Slide 27: Influence of load ratio
da/dN
DK
Low R value (typically 0.1)
R increasing
When R increases:
- da/dN increases for a fixed value of K;
- KThreshold decreases.

## Slide 28: Crack closure
DK
Open crack
Partially closed crack
Keff
Hyp : a crack can propagate only when it is fully open  da/dN fonction of Keff
Elber (1970):
Experimental evidence that a fatigue crack , even when loaded in tension (R>0) can be partially closed during the lower part of the loading cycle.
For the 2024 T351 alloy in Paris regime:

## Slide 29: Crack closure sources
Plastic wake
contact
Residual
mode II displacement
Plasticity induced closure
Formation of a thick oxide layer  “wedge” effect”
Oxide induced closure
Roughness induced closure

## Slide 30: Plasticity-Induced Closure
The material flow from the bulk that accumulates on the crack flanks, thereby giving rise to the premature contact as noted by Sun and Sehitoglu

## Slide 31: Roughness-Induced Closure
Garcia and Sehitoglu modelled roughness-induced crack closure as a contact problem with random distribution of surface asperities.

## Slide 32: Opening kinematics
FEM Simulation of the crack opening in a CCT specimen (after Chermahini et al. 1988 ).

## Slide 33
Experimental measurement of the crack opening load
d
P
Back-face strain gage
P
d
Compliance of open crack
Compliance of the partially closed crack

## Slide 34: Experimental measurement of the crack opening load

## Slide 35: Influence of metallurgical parameters
Grain size
K eff,th
ARMCO iron
The coarser the grain, the higher the threshold ↔ crack closure effect
K eff, th (air)
K eff, th (vac)
Yield strength
The higher the yield strength, the lower the threshold ↔ crack closure effect

## Slide 36: Influence of environment
A moist environment induces a loss of resistance

## Slide 37: Propagation assistée par l’hydrogène
Transport
 accès des espèces actives en pointe de fissure
 adsorption physique
 adsorption chimique et dissociation
 pénétration et diffusion de l’hydrogène en pointe de fissure
Réaction de fragilisation
M
H
H

## Slide 38: Fatigue Crack Propagation Laws
Empirical Laws:
Theoretical approaches:
Paris
Forman
CTOD (Pelloux)
Manson-Coffin at the crack tip (McClintock, Antolovitch,…)
Cumulative damage at the crack tip

## Slide 39: Intrinsic fatigue crack growth (inert,DK eff)
1
4
1
4

## Slide 40: Short cracks
da/dN
a (crack length) or DK
Long cracks
Natural short cracks
Short cracks from notches
Absence of threshold
Def : cracks for which at least one dimension is small with respect to other dimensions (geometry, grain size,…)

## Slide 41: Kitagawa diagram
log()
log (a)
1
2
ac
Non failure
Failure
D

## Slide 42: Kitagawa Diagram